LYTHIC FLOOR PROTECTOR

PERFORMANCE SPECIFICATION FOR Polishing using the Lythic PROTECTOR system –
This specification is provided as a service and is intended to be used as a guideline for preparing the appropriate project specific specification sections.

The quality and level of Diamond Polishing is always the starting point of a good polished floor.

EXECUTION

Complete all floor prep including densification, coloring, and polishing before applying Lythic Protector. Clean floor to remove dust and debris. The surface should be completely clean and dry before application.

APPLICATION

Lythic Protector is recommended, as a contaminant barrier and to increase the shine and depth of colour.

Surface should be completely clean and dry before application of Lythic Protector.

Using a low-pressure pump sprayer, apply Lythic Protector in a light mist. Using a damp micro fibre or flat cotton pad applicator, spread Lythic Protector in a thin film coat using a figure 8 motion to reduce streaking and to prevent puddling.

Once completely dry use floor stripper pads to smooth out the Protector barrier (Black Stripper Pad) Then burnish with Hogshair pad or similar/ OR use diamond impregnated pads will do the same as the 2 step process as described above.
Burnishing with a minimum 2000 RPM machine.

For this burnish achieve a concrete surface Temp of 32C. A hand held digital temperature device is ideal for this purpose and can be purchased from Jaycar 16-18 Fisher Crescent Mt Wellington, Ph. 0800 452 922 model number is QM7215 

Allow finished floor to cure for 24 hours before allowing regular foot traffic. Wait 72 hours before leaving standing water. Protector is only for Indoor usage.

Cure finished floor for 24 hours before allowing regular foot traffic. Do not allow standing water to remain on the surface for the first 72 hours. 
Reapplying Protector and burnishing can renew the shine.

www.concretesealers.co.nz