LYTHIC FLOOR SPD PROTECTOR

This specification is provided by Lythic Solutions as a service and is intended to be used as a guideline for preparing the appropriate project specific specification sections.

PERFORMANCE SPECIFICATION FOR Polishing using the Lythic Exposed Aggregate Floor system

EXECUTION

SURFACE CONDITIONS:

Examine substrate for conditions affecting performance of finish.

Correct conditions detrimental to timely and proper work. Do not proceed until unsatisfactory conditions are corrected.

A. Verify that base slab is clean of	any mastic	or adhesives from previous floor coverings, loose debris, dirt, mildew, oils and grease and efflorescence, curing and latent construction materials.

B.  New concrete must be in place a minimum of 28 days or as directed by the

Manufacturer before application can begin.

APPLICATION

A. Floor to be prepared for Lythic Densifier application with sanding screens or diamond tooling as needed to remove contaminants. Polish level to be determined by test samples provided on‐site.

B.  Floor to be sealed with Lythic SPD Protector after diamond polishing to prevent staining   and acid etching.

C. Hardening, Polishing and sealing, of Concrete Surface

1. Applicable procedures must be followed as recommended by the product manufacturer and as required to match approved test sample.

2. Achieve dust-proofing and abrasion resistance of the surface without changing the

natural appearance of the concrete, except for the sheen.

3.  Seal to protect surface from acid etching and staining.

4. Finish to within 12mm of vertical surfaces where practical.

5. Level of polish based on test sample.

D. FINAL PROTECTION
Following completion of the final polishing, surface must be covered to protect from other trades. Cover with breathable product, such as kraft paper,  “Ram Board”.Do not cover with rosin paper. Plywood protection to have 4 mil plastic slip sheet barriers between wood and slab.

www.concretesealers.co.nz