As the technology of Colloidal Silica bonds with itself, a property not seen in any other product.

This allows a slab treated with DAY1 be burnished to produce a permanently Densified, Dust Proofed, Abrasive Resistant floor with a Shine. This ceates a slab with great aesthetics and ease of cleaning at a Low Cost with NO Grinding using the Lythic Hardwear Floor process.

DAY1 provides an ideal substrate to receive polishing/burnishing using the Lythic Hardwear Floor or Exposed Aggregate system.

The Hardwear Floor is a Breakthrough Technology that provides a Densified, Dust Proofed, Abrasive Resistant floor with a Shine.

There are 2 application protocols to achieve a Hardwear Floor on a slab treated with DAY1 as follows:

Option 1:
Apply Lythic XL Densifier directly after pour.
After 21 – 28 days clean and burnish.
You can proceed to test burnish at an earlier date, say after 5 days. Burnish with minimum 2000 RPM machine
Apply Lythic Protector as an option to increase shine and stain resistance.

Option 2:
After 21 – 28 days Clean slab with water
Apply Lythic XL Densifier
Burnish with minimum 2000 RPM machine
Apply Lythic Protector as an option to increase shine and stain resistance

Exposed Aggregate (polished floor)

To polish a slab treated with DAY1 protocol is as follows:
After 21-28 days proceed with standard Lythic Polishing protocols.

www.concretesealers.co.nz